## Slide 1: 06/28/2024 A Review of Photogalvanic Effect
Review of SHG(we could skip it)
Photogalvanic: Perturbation theory
Defect states
Defects, Oxygen Vacancy, exact contributor to defect states
Resonator case(see if time permits)

## Slide 2: Nonlinear Optics Reaction in General
Constraint 1:
Constraint 2:
Phase Match ≡ Meet both constraints at the same time

## Slide 3: Second Harmonic Generation and χ(2)
z
  Can‘t happen in centrosymmetric material(material with one refractive index)
  Requires material to be birefringent(non-zero χ(2))

## Slide 4: Solve the amplitude of 2nd harmonics: f(z)
The wave equation with χ(2) nonlinearity:
Assumptions:
  1:
  2: Only SHG happens(other second order reactions does not)
  3:

## Slide 5: The solution
χ(2)
  2nd harmonics power
    χ(2)
    Pump intensity
    Phase ”δ”

## Slide 6: Quasi Phase Match
  It is hard to match phase perfectly
  When the phase misalignment goes above a threshold:
    Oscillation between |w> and |2w> happens
    SHG efficiency drops
  In LiN, Quasi-Phase Match:
    Manually flip the phase periodically by engineering the material

## Slide 7
If material has no χ(2) naturally,
can I still generate SHG in it?
Notes: Centrosymmetric
Hard to do phase match

## Slide 8: Susceptibility in tensor notation
χ(n) is an (n+1) tensor
From pure tensor contraction:
  χ(2)fake = χijkfake = χijkl El
  χ(2) could be constructed by any (2+n) tensor with n static E-field
  Contribution from χ(2) dominates:

## Slide 9: First Observation of SHG in glass fiber
Osterberg U, Margulis W Opt. Lett. 11 516 (1986)
O Yakar, E Nitiss, J Hu, CS Brès Laser & Photonics Reviews, 2022

## Slide 10: Observed 2nd Harmonics in SiN waveguide
SHG, red light
THG, green light
1539 nm (magenta line), 1544 nm (blue line) and 1549 nm (black line).
Pink = 1539 nm
Blue = 1544 nm
Black = 1549 nm
Notes: In fact, green photons with a ~2.4 eV energy are able to directly re-ionize the electrons trapped in acceptor states below the conduction band28. Such a linear absorption process does not lead to any preferential emission and the electrons just move accordingly to the EDC, opposite to the direction of the photogalvanic current. Moreover, CPE can also involve multi- photon coherent interference from one pump photon and one photon at the THG frequency, albeit with the wrong periodicity. We therefore ascribe the oscillations observed during the growth of SHG in waveguide (i) to the counter-acting effects of CPE involving photons from THG and direct re-ionization also due to third harmonic photons.

## Slide 11
If the grating is spatially periodic
what could be the E field that contributes to it?
  χ(2)fake = χijkfake = χijkl El

## Slide 12: Spatially Periodic Charge Separation
O Yakar, E Nitiss, J Hu, CS Brès Laser & Photonics Reviews, 2022
A Billat, D Grassani, MHP Pfeiffer, S Kharitonov, TJ Kippenberg, CS Brès
Nature communications, 2017

## Slide 13: Jargon Definition(This is just a menu.)
  Illuminate := Use a light to shoot your sample
  Fundamental := |w>
  Pump := |w>
  Second harmonics wave := |2w>
  Trap Site := Defect state
  Write := Action to produce χ(2)fake grating. Typically mean : Use |w,1064> and |2w,523> to illuminate a sample
  Read := Action to generate SHG |2w>. Typically mean use |w,1064>. To illuminate a sample
  Erase := Action to remove χ(2)fake grating. Typically mean: Use |2w, 523> to illuminate a sample
  Seeding :=Action to produce χ(2)fake grating. Specifically mean to use |w,1064> and |2w,523> to illuminate a sample
  Defect := locally does not obey crystal symmetry
  Defect State := eigenstate for the local Hamiltonian(Depends on how strong the local Hamiltonian coupled to the environment )
  Configuration := the geometry of the bonds and atoms

## Slide 14: Charge Separation: Photogalvanic Effect
A quantum model
Quantum Interference(cross term) among different paths
Perturbation applied to 4th order(otherwise can’t see it)
Uneven transition rate
Donor: (lower energy level defect)
  Defect state 1(Trap site)  Conduction band
Receiver: (higher energy level defect)
  Conduction band   Defect state 2(not shown here)
For glass
DZ Anderson, V Mizrahi, JE Sipe Optics letters, 1991•opg.optica.org
Notes: Quantum interference (product term in n-th order perturbation coefficients)
Recent evidence4 suggests that the induced x()) is in fact the result of some internal dc e1ectrie field acting on there J) of the glass
Such a de electric field would perhaps come from charges released from certain defect sites in the glass, and trapped at other sites. This picture has been suggested by several worker

## Slide 15: Photogalvanic Effect: Charge Transport Model
Difference: Charge in the conduction band
V0: Initial speed when kicked out
Τm : Time when exciton decoheres
Sum: Electron holes both will move under E
nd: density of sites
ΤR : Time when electron is trapped again
Ohmic: J = б E
Just a capacitor
Help: why omic necessarily?

## Slide 16: An Analogy
This is a classical capacitor
Defect State with lower energy(e donor)
Defect State with higher energy(e receiver)
CB
-
-
+
+
-
+
This is a quantum version capacitor

## Slide 17: Another Analogy—Global/local electron Trap
A random picture of a band diagram that contains a global and local trap I found from some molecular computational physics journal

## Slide 18
What do I mean by “defect”?

## Slide 19: Jargon definition
  Defect := locally does not obey crystal symmetry
  Defect State := eigenstate for the local Hamiltonian(Depends on how strong the local Hamiltonian coupled to the environment )

## Slide 20: What do I mean by “defect”?: Example 1
Popular belief:
The defect in SiN is from vacancy
VA Gritsenko, TV Perevalov, OM Orlov… - Applied Physics …, 2016 - pubs.aip.org
For SiN
They call it “Memory Effect”
  Defect := locally does not obey crystal symmetry
  Defect State := eigenstate for the local Hamiltonian

## Slide 21: What do I mean by “defect”?: Example 1
Oscillation:
1. |1500> | 750> are writing (writing means sending electrons to the prison)
2. |500> is erasing (erasing means helping trapped electrons to escape)
3. They are fighting against each other
Pink = 1539 nm
Blue = 1544 nm
Black = 1549 nm

## Slide 22: What do I mean by “defect”?: Example 2
JM Gabriagues, H Fevrier - Optics letters, 1987 - opg.optica.org
Some crazy theorist uses “ring” topology to argue for defect
GeO2-related defects
Will specifically expand more from the perspective of oxygen vacancy later,
as defects in GeO2 are crucial to our project
Notes: Trapping Mechanism and Persistence
Trapping in SiN: In SiN, nitrogen vacancies saturated with hydrogen atoms (leading to Si–H and Si–Si bonds) act as traps for both holes and electrons.
Trap Energies: Electron and hole traps are located inside the ~4.6 eV bandgap of SiN, around 1.4 eV from the conduction and valence bands, respectively.

## Slide 23
As we currently do not see SHG in the resonator,
what could be the reason from the bandgap side?

## Slide 24: Trap site for GeO2-SiO2
NB
CB
9 ev
Defect 1
3.8 ev
5.1 ev
Data obtained by Haojing and fitted by me
Notes: matched χ(2)\chi^{(2)}χ(2) grating in the fiber (L2ω∝A2P0nL_{2\omega} \propto A^2P_0^nL2ω​∝A2P0n​), and then some of this light is absorbed through two-photon absorption (∝P02\propto P_0^2∝P02​). This TPA would, in this picture, result in the release of the trapped charges which are responsible for the internal macroscopic dc field that gives rise to the χ(2)\chi^{(2)}χ(2). Since the effect is almost absent in fiber B, we presume that such TPA is germania related. Note that the erasure process of Ouellette et al., described by Eq. (1), which is quartic in the green power as compared with our quadratic dependence, is ignored in Eq. (2) due to the relative weakness of the generated SH, as compared with the seed green intensity.
A broad linear absorption band centered at 245 nm is known to exist in germania glass, and is well placed for TPA of the 532 nm light. While the defect structure responsible for this band is still the subject of discussion, it is considered to be due to an oxygen vacancy neighboring a Ge atom. This therefore suggests that the origin of the decay might be related to the local environment of the Ge atoms. Bonds such as −Ge−Ge−-Ge-Ge-−Ge−Ge− or −Ge−Si−-Ge-Si-−Ge−Si− are weaker than other bonds in silica glass (such as −Si−O−Si−-Si-O-Si-−Si−O−Si−), and may therefore be more easily affected by TPA of the 532 nm light. Furthermore, it should be noted that while the 1064 nm and 532 nm light together can create the SHG grating, the 1064 nm light alone erases the SHG grating in fiber A. For the SHG from irradiated fibers to be a function of the IR power, the grating has to be stable over the writing period.
The slope of the curves from 2(b), plus additional data vs 1064 nm power used during the reading phase of fiber A. The solid line is the result of a linear least-squares fit.
In conclusion, we have investigated SHG in a high germania content fiber, seeded with Q-switched mode-locked pulses at 532 and 1064 nm. The SHG from the fiber was observed to decay upon exposure to 1064 nm light alone, which we have not observed over short times in fibers with low GeO2 content. The decay rate was proportional to the fourth power of the 1064 nm power, which is consistent with a model based on TPA of the generated SH light. This result suggests that the germania is important in the decay. To obtain more stable SHG in fibers, and to understand its formation mechanism, it appears necessary to investigate the SHG of optical fibers with various GeO2 concentrations.
This research was supported by the Air Force Office of Scientific Research under AFOSR-87-0344, and by NTT laboratories. We wish to thank M. Shimizu of NTT laboratories for providing fiber B.

## Slide 25: Trap site for GeO2-SiO2
NB
CB
9 ev
Defect 1
3.8 ev
5.1 ev
Popular belief: Oxygen Vacancy around the Ge atom
(Think of it as a capacitor, I need someone to lose and someone to gain, to form charge separation)
Donor does not donate electrons :
  What is Defect 1?
  Can I engineer it to make it closer to conduction band?
Receiver failed or too easy to lose electrons:
  What is Defect 2?
  What is its density?
  How easily is it to excite electrons away from it?
Notes: matched χ(2)\chi^{(2)}χ(2) grating in the fiber (L2ω∝A2P0nL_{2\omega} \propto A^2P_0^nL2ω​∝A2P0n​), and then some of this light is absorbed through two-photon absorption (∝P02\propto P_0^2∝P02​). This TPA would, in this picture, result in the release of the trapped charges which are responsible for the internal macroscopic dc field that gives rise to the χ(2)\chi^{(2)}χ(2). Since the effect is almost absent in fiber B, we presume that such TPA is germania related. Note that the erasure process of Ouellette et al., described by Eq. (1), which is quartic in the green power as compared with our quadratic dependence, is ignored in Eq. (2) due to the relative weakness of the generated SH, as compared with the seed green intensity.
A broad linear absorption band centered at 245 nm is known to exist in germania glass, and is well placed for TPA of the 532 nm light. While the defect structure responsible for this band is still the subject of discussion, it is considered to be due to an oxygen vacancy neighboring a Ge atom. This therefore suggests that the origin of the decay might be related to the local environment of the Ge atoms. Bonds such as −Ge−Ge−-Ge-Ge-−Ge−Ge− or −Ge−Si−-Ge-Si-−Ge−Si− are weaker than other bonds in silica glass (such as −Si−O−Si−-Si-O-Si-−Si−O−Si−), and may therefore be more easily affected by TPA of the 532 nm light. Furthermore, it should be noted that while the 1064 nm and 532 nm light together can create the SHG grating, the 1064 nm light alone erases the SHG grating in fiber A. For the SHG from irradiated fibers to be a function of the IR power, the grating has to be stable over the writing period.
The slope of the curves from 2(b), plus additional data vs 1064 nm power used during the reading phase of fiber A. The solid line is the result of a linear least-squares fit.
In conclusion, we have investigated SHG in a high germania content fiber, seeded with Q-switched mode-locked pulses at 532 and 1064 nm. The SHG from the fiber was observed to decay upon exposure to 1064 nm light alone, which we have not observed over short times in fibers with low GeO2 content. The decay rate was proportional to the fourth power of the 1064 nm power, which is consistent with a model based on TPA of the generated SH light. This result suggests that the germania is important in the decay. To obtain more stable SHG in fibers, and to understand its formation mechanism, it appears necessary to investigate the SHG of optical fibers with various GeO2 concentrations.
This research was supported by the Air Force Office of Scientific Research under AFOSR-87-0344, and by NTT laboratories. We wish to thank M. Shimizu of NTT laboratories for providing fiber B.

## Slide 26: Trap site for GeO2-SiO2
Y Hibino, V Mizrahi, GI Stegeman, S Sudo - Applied physics letters, 1990 - pubs.aip.org
Fiber A: High concentration GeO2 fiber
Fiber B: Low concentration
Both written by |1032> + |532> for 1.5h
High concentration leads to erasure even during reading(|1064>)
High concentration + high power = giga quick erasure of your grating during reading
B
A
A
A
A

## Slide 27: Trap site for GeO2-SiO2
Y Hibino, V Mizrahi, GI Stegeman, S Sudo - Applied physics letters, 1990 - pubs.aip.org
  This is an old paper, but it does point out that:
  The defect is related to GeO2
B
A
A
A
A

## Slide 28: 5GeO2-95SiO2
5ev
J Nishii, K Fukumi, H Yamanaka, K Kawamura, H Hosono, H Kawazoe
Physical Review B, 1995•APS

## Slide 29: Jargon Definition 2
NOMV := Neutral Oxygen Monovacancy ; Donor ; absorb 5 ev
NODV := Neutral Oxygen Divacancy ; Donor ; emit 3.2/4.3 ev
Ge E’ := Germanium E' Center; Oxygen-deficient center; Donor; absorb 6.4ev
GEC := Germanium Electron Center ; receiver ; absorb 4.4/5.8 ev
GLPC := germanium atom with a lone pair of electrons ; recever ; 5.16 ev

## Slide 30: Defect State for GeO2-SiO2
J Si, K Kitaoka, J Qiu, T Mitsuyu, K Hirao Optics letters, 1999•opg.optica.org
5.7
4.7
6.3
5.1
before
after
J Nishii, K Fukumi, H Yamanaka, K Kawamura, H Hosono, H Kawazoe
Physical Review B, 1995•APS
As shown in Fig. 3, some new bands located near 4.7, 5.7, and 6.3 eV were induced after the SHG preparation, which are assigned, respectively, to the absorption of a Ge electron trapped center (GEC) [Ge(1) or Ge(2)] and a GeE0 center of 10-GeO2 90-SiO2 glasses based on earlier studies.16

## Slide 31: People’s understanding(1995)
J Si, K Kitaoka, J Qiu, T Mitsuyu, K Hirao - Optics letters, 1999 - opg.optica.org
Defect state as donor:
Defect state as receiver:

## Slide 32: People’s understanding keeps updating(1999)
J Si, K Kitaoka, J Qiu, T Mitsuyu, K Hirao - Optics letters, 1999 - opg.optica.org
GeE' Center: Neutral, oxygen-deficient, and formed as incidental defects.
GEC: Negatively charged, electron-trapped centers formed through intentional excitation and trapping processes.
This is still a postulation

## Slide 33
What is Defect 1(Donor)? Lone Pair in Bridging Oxygen
What is Defect 2(Receiver)? GeO4 ‘s Ge

## Slide 34: Trap site for GeO2-SiO2
NB
CB
9 ev
Defect 1
3.8 ev
5.1 ev
Popular belief: Oxygen Vacancy around the Ge atom
Donor does not donate electrons :
  What is Defect 1? There are two defects states: Ge(1) and Ge(2). Ge(1),4.7ev, is from Electron Pair in Bridging Oxygen
  Can I engineer it to get it closer to the conduction band?
Receiver failed or too easy to lose electrons:
  What is Defect 2? GeO4 ‘s Ge
  What is its density?
  How easily is it to excite electrons away from it?
Notes: matched χ(2)\chi^{(2)}χ(2) grating in the fiber (L2ω∝A2P0nL_{2\omega} \propto A^2P_0^nL2ω​∝A2P0n​), and then some of this light is absorbed through two-photon absorption (∝P02\propto P_0^2∝P02​). This TPA would, in this picture, result in the release of the trapped charges which are responsible for the internal macroscopic dc field that gives rise to the χ(2)\chi^{(2)}χ(2). Since the effect is almost absent in fiber B, we presume that such TPA is germania related. Note that the erasure process of Ouellette et al., described by Eq. (1), which is quartic in the green power as compared with our quadratic dependence, is ignored in Eq. (2) due to the relative weakness of the generated SH, as compared with the seed green intensity.
A broad linear absorption band centered at 245 nm is known to exist in germania glass, and is well placed for TPA of the 532 nm light. While the defect structure responsible for this band is still the subject of discussion, it is considered to be due to an oxygen vacancy neighboring a Ge atom. This therefore suggests that the origin of the decay might be related to the local environment of the Ge atoms. Bonds such as −Ge−Ge−-Ge-Ge-−Ge−Ge− or −Ge−Si−-Ge-Si-−Ge−Si− are weaker than other bonds in silica glass (such as −Si−O−Si−-Si-O-Si-−Si−O−Si−), and may therefore be more easily affected by TPA of the 532 nm light. Furthermore, it should be noted that while the 1064 nm and 532 nm light together can create the SHG grating, the 1064 nm light alone erases the SHG grating in fiber A. For the SHG from irradiated fibers to be a function of the IR power, the grating has to be stable over the writing period.
The slope of the curves from 2(b), plus additional data vs 1064 nm power used during the reading phase of fiber A. The solid line is the result of a linear least-squares fit.
In conclusion, we have investigated SHG in a high germania content fiber, seeded with Q-switched mode-locked pulses at 532 and 1064 nm. The SHG from the fiber was observed to decay upon exposure to 1064 nm light alone, which we have not observed over short times in fibers with low GeO2 content. The decay rate was proportional to the fourth power of the 1064 nm power, which is consistent with a model based on TPA of the generated SH light. This result suggests that the germania is important in the decay. To obtain more stable SHG in fibers, and to understand its formation mechanism, it appears necessary to investigate the SHG of optical fibers with various GeO2 concentrations.
This research was supported by the Air Force Office of Scientific Research under AFOSR-87-0344, and by NTT laboratories. We wish to thank M. Shimizu of NTT laboratories for providing fiber B.

## Slide 35: ab initio quantum-chemical calculations—different model
T Uchino, M Takahashi, T Yoko - Physical Review Letters, 2001 - APS

## Slide 36: For the remaining questions
I need more time and more wisdom from others
If we could engineer the material, to get a band diagram we want.
  I.e. if we want to do it at 1550, could we engineer it, to obtain two defect states as a capacitor?
  I.e. if we fail to see it under 1064, could we engineer it,
  to make the two defect states favor our reaction?

## Slide 37: I cite this one from Haojing’s slide
532nm out
Microring
U taper
WDM
1064nm in
532nm in
WDM
1064nm out
1064nm: pump, write grating
532nm: seed, monitor resonance match
Heater: align resonances of two wavelength
2022 Nature Photon.
Quasi-phase-matching photo galvanic SHG
Heating by TEC

## Slide 40: Jargon Definition 2
NOMV := Neutral Oxygen Monovacancy ; Donor ; absorb 5 ev
NODV := Neutral Oxygen Divacancy ; Donor ; emit 3.2/4.3 ev
Ge E’ := Germanium E' Center; Oxygen-deficient center; Donor; absorb 6.4ev
GEC := Germanium Electron Center ; receiver ; absorb 4.4/5.8 ev
GLPC := germanium atom with a lone pair of electrons ; recever ; 5.16 ev
5GeO2-95SiO2

## Slide 41: 07/12/2024
Comsol Simulation-Group Velocity Matching
Measure lens fiber coupling efficiency
Pump the waveguide with MZM + YDFD (no green light still)
TEC
Tsunami

## Slide 42: Comsol Simulation – Confirm it with published data in SiN
650*1970 nm

## Slide 43: Comsol Simulation – GeO2-SiO2
FHD
Ge-SiO2 (2% doping RTA) (Shijia-UCSB 2024a: n 0.459-1.688 µm)
None of them matches the GVD.
Simulation is wrong
In fiber they do see green light, does fiber meet GVD?

## Slide 44: Measure lens fiber coupling efficiency
We currently have:
  2 x 1550nm lens fiber
  0 x 1064 lens fiber
We need to purchase
  4 x 1550nm lens fiber, spot size = 5um
  4 x 1064nm lens fiber, spot size = 5um(undetermined)
  Roughly 90 dollar each
https://www.ozoptics.com/ALLNEW_PDF/DTS0080.pdf
The best combo now is 5um spot size + 8um waveguide

## Slide 45: Pump the waveguide with MZM + YDFD
No green light
Pumped for 4hrs
Power still too weak(8mw after 25db)

## Slide 46: Thermoelectric cooler(TEC)
  Old TEC cannot converge and heats up extremely quickly
  Unable to measure Qabs
  The unused TEC we have is too small and unsuitable for Qabs measurement
  I still made one based on the small TEC but it takes a year to converge to the setpoint

## Slide 47: Tsunami – Current Hunting results
  Boxes for ND filter but only boxes
  0 x Isolator
  0 x Beam Dump

## Slide 48: Things to purchase for Tsunami
<Tsunami Power> = 2W
1 x ND kits(79% to 0.01%)
1 x Beam Dump
1 x cover
Isolator is too expensive, and I want to try to find one first

## Slide 49: Overall
8 x lens fiber (4 for 1064/ 4 for 1550)
4 x TEC_H3S
1 x Beam Dump
1 x ND filters
1 x cover for Tsunami Safety
Stages or mounts if necessary
Need to find one isolator

## Slide 50: 07/18/2024

## Slide 51: Setup
Ti: Sapphire
Waveguide/Spiral/Ring
x 40 lens
λ/2 Waveplate
Polarization
Beam Splitter
P-polarized
S-polarized
Beam Dump
AR Coating: 400-700nm
Numerical Aperture v.s. waveguide NA
Backscattering
x 60 lens
x 20 lens
We have it, and its parameters match
We have it, but its parameters don’t match
We don’t have it
See later slides
Average power: 2W
Peak power: 312.5kW
Pulse energy = 25nJ
Repetition rate = 80MHz
Act as an attenuator

## Slide 52: What kind of measurements’ tool we want?
If fiber:
Ti: Saphh
Waveguide/Spiral/Ring
x 40 lens
λ/2 Waveplate
Polarization
Beam Splitter
P-polarized
S-polarized
Beam Dump
AR Coating: 400-700nm
Numerical Aperture v.s. waveguide NA
Backscattering
x 60 lens
x 20 lens
If free space:
Lens Fiber +V groove
We only have two left, and Peng will also use it
I want five more
OSA(300-1000nm)
We have it, and its parameters match
We have it, but its parameters don’t match
We don’t have it

## Slide 53: Summary of what I want to buy
5 x lens fiber
1 x blackout
1 x V groove(For fiber dangling in the air)
If pulses coming out of the waveguide are still too strong, there is a specific component for femtosecond pulse attenuation:
Lead time = 2 weeks

## Slide 54: Replicate NC simulation result
0.826
1.06
1.69

## Slide 55: Miscellaneous
Can I take things away from NTT stage?
Final report date(I want to work longer!)

## Slide 56: 1064nm Absorption Q results
Use a degraded device as a test, (3mm ring with 6um width)
(use a FHD ring results @1550nm,
waiting new TEC for remeasurement)
1064 taper transmission > 97.5%
Need unattach taper to reduce scattering loss
Use less mode cavity as possible

## Slide 57
Mode Lock Controller
A box containing Ti:Sapphire
CW
CW Controller
Optical Parametric Oscillator(Not used)

## Slide 58
Two lines that deliver the coolant

## Slide 60
Press this

## Slide 66: 2024/07/26
Ti: Saphh
Waveguide/Spiral/Ring
λ/2 Waveplate
Polarization
Beam Splitter
P-polarized
S-polarized
Beam Dump
x 60 lens
Integrating
Sphere

## Slide 67: Current Setup
Effective Couple

## Slide 68: Current Setup
Waveguide, 4um x 6um cross section
, Air cladded
GeO-SiO2
4um
6um
Si

## Slide 69: Edge
Damage due to pulse laser

## Slide 70: Giga confused by the German result
Mine
German’s
Mine

## Slide 73: 2024/07/31
Skipped

## Slide 74: Substrate v.s. height determine where the mode resides

## Slide 76: 2024/08/09

## Slide 77: Vary Base Thickness, Waveguide Height, and Width Comsol Cross Section For Width/High = 2 is Shown
2
Height/Width =2
2
2
1
2
2

## Slide 78
2
2
2
2
2
2
1
1

## Slide 79: Promising candidate
Vary width from 0.5um to 3.6um
Substrate thickness 500nm or 750nm (or 250nm, this might be too thin)
Waveguide height 500nm or 1000nm

## Slide 80: Layer1 for MLA

## Slide 81: Layer2 for MLA

## Slide 82: Edge Couple Setup
Pin = 1W
Best record: Pout = 200mw(not stable)
Normally: Pout =20mw(could last for 4hours)

## Slide 83: Waveguide and Spiral
Nc Super Continuum paper: 2300pj, 30% 690
My for 20mw: 35 000pj, 1%350

## Slide 84: Reduce spot size